## Slide 1
Measurement Model Examples
Notes: Here we will look at some comparisons of measurement model predictions with measured signals.

## Slide 2
Learning Objectives
Comparison of the measured signals and the signals predicted by a measurement model for three common reference reflectors:
spherical pore
flat-bottom hole (flat crack)
side-drilled hole
Notes: To see the quality of the signals predicted by our ultrasonic measurement models in comparison with actual experimental signals, we have shown some time domain responses for three types of commonly used reference reflectors.

## Slide 3
50.8
mm
19.63
mm
(a)
(b)
0
1
2
3
4
5
6
7
8
9
10
-2.5
-2
-1.5
-1
-0.5
0
0.5
1
1.5
2
x 10
-3
time, msec
output, volts
time, msec
0
1
2
3
4
5
6
7
8
9
10
-0.8
-0.6
-0.4
-0.2
0
0.2
0.4
0.6
output (volts)
0
2
4
6
8
10
12
14
16
18
20
0
0.01
0.02
0.03
0.04
0.05
0.06
0.07
0.08
frequency, MHz
s(f) volts/MHz
Spherical Pore
Thompson-Gray Measurement Model
(1)
(2)
(3)
Notes: (1) The measurement model results for the pulse-echo response of a 0.6921 mm diameter spherical void, using the Thompson-Gray measurement model and the Kirchhoff approximation for the scattering amplitude. (2) The system function, as measured in setup (a), for the 12.7 mm diameter, 5 MHz transducer used. (3) A comparison of the measurement model signal (solid line) with the experimentally measured signal (dashed line).

## Slide 4
50.8
mm
25.4
mm
(a)
(b)
50.8
mm
25.4
mm
Flat-bottom hole or flat crack at normal incidence
“Large” flaw measurement model
0.5
1
1.5
2
2.5
3
3.5
4
4.5
5
-0.02
-0.015
-0.01
-0.005
0
0.005
0.01
0.015
0.02
time, msec
output, volts
Notes: The measurement model results for the pulse-echo P-wave response of a 1.5875 mm radius flat-bottom hole (which also looks like a flat crack), where the system function was measured as in the previous case and the variation of the amplitude of the incident waves over the flat-surface was taken into account in the Kirchhoff approximation (Highly specular reflectors, like a flat-bottom hole or flat crack, are more sensitive to the small flaw assumption than are reflectors like the spherical pore just considered) . Shown is a comparison of the measurement model signal (solid line) with the experimentally measured signal (dashed line).

## Slide 5
50.8
mm
25.4
mm
(a)
(b)
Side-drilled Hole
2-D Measurement Model
0
1
2
3
4
5
6
7
8
9
10
-0.02
-0.015
-0.01
-0.005
0
0.005
0.01
0.015
0.02
0.025
time, msec
outputs, volts
Notes: Comparison of the measurement model predictions for the pulse-echo P-wave response of a 1 mm diameter side-drilled hole with a 5MHz transducer (solid line) with the experimentally measured signal.