## Slide 1
Wave Propagation Fundamentals -3
Ultrasonic Attenuation
Notes: Waves propagating in real material will experience attenuation due to a number of sources. Our discussion of wave propagation so far has ignored attenuation so we will now look at some methods for including this attenuation in our models.

## Slide 2
Learning Objectives
Attenuation definitions
Simple method for measuring average attenuation
Model-based approach for determining attenuation
as a function of frequency
Notes: We will give a very simple method for obtaining an average attenuation value for a material and describe a more detailed approach that will allow us to include a frequency dependent attenuation in wave propagation and wave scattering calculations.

## Slide 3
Ultrasonic Attenuation
A1
A2
attenuating
medium
d
attenuation (Np/unit length)
plane wave amplitudes:
Notes: Attenuation in real materials is a complex process. Attenuation may be due, for example, as a result of the scattering of waves from the small grains that exist in a material, thus reducing the amplitude of a propagating wave. In our models of wave propagation we will not try to describe those attenuation processes in detail. Instead, we will use a simple plane wave model where will assume that the attenuation effects can be included by multiplying the wave amplitudes obtained for an ideal (on-attenuating) medium by an exponential decaying factor containing a frequency dependent attenuation coefficient and the distance of propagation. The attenuation coefficient is measured in Nepers/unit length where a Neper (Np) is a non-dimensional quantity.

## Slide 4
John Napier of Merchistoun (1550 – 4 April 1617), nicknamed Marvellous Merchistoun, was a Scottish mathematician, physicist, astronomer/astrologer and 8th Laird of Merchistoun. He is most remembered as the inventor of logarithms and Napier's bones, and for popularizing the use of the decimal point. Napier's birth place, Merchiston Tower, Edinburgh, Scotland, is now part of Napier University. He is buried in St Cuthbert's Church, Edinburgh
Notes: Here is a short description of Napier. The Neper unit is derived from his name.

## Slide 5
Example: water
Attenuation is affected by many variables so that
generally it is not possible to give generic values
that are useful for quantitative analyses.
Thus, attenuation generally must be obtained
experimentally for the material in question
When attenuation values are quoted they are often
given as average values in decibels/unit length
f … Hz
Notes: We can easily measure the attenuation coefficient in water as a function of frequency. The result is shown above, where we see that the attenuation increases like the square of the frequency. Here the attenuation coefficient is given in Nepers/meter and the frequency, f, is measured in Hertz (Hz). For other materials it is not possible to give similar generic results since the attenuation is controlled by many aspects of how the material is manufactured and it is usually necessary to measure the attenuation on a sample of the material being used. Attenuation values are also often quoted in terms of decibels/ unit length but the conversion from Nepers/unit length to decibels/unit length is simple, as shown (see the next slide for how this conversion is obtained).

## Slide 6
A2
A1
average attenuation (Np/l)
average attenuation (dB/l)
d
plane wave
pulse traveling
in an attenuative
medium:
Notes: One can measure the amplitude changes of a waveform over a distance and determine an average attenuation for the material. This attenuation can also be expressed in either Nepers/unit length or dB/unit length. We need a more detailed measure of the attenuation as a function of frequency to include in our ultrasonic models but a measurement of the average attenuation can give us a rough indication of the importance of attenuation in a material.

## Slide 7
To model the effects of attenuation on the characteristics of a signal, we must be able to find the attenuation of a material as a function of frequency. However, in some applications we may be content to obtain an average attenuation value which describes the overall behavior of the amplitude of the signal. We can obtain such the average attenuation of a solid sample, for example, by using the pulse-echo setup shown.
D
On the oscilloscope screen we will see a series of evenly spaced pulses that are decreasing in amplitude. These are the waves that have been reflected from the back surface of the block one or more times.
Simple method to determine average attenuation
Notes: If all we are interested in is the effects of attenuation on the signal amplitude, we can use a very simple pulse-echo measurement to obtain the average attenuation. We place a transducer on a block of the material and examine the waves that are reflected one or more times from the back surface.

## Slide 8
A1
A2
A3
A4
Let the measured amplitudes of these signals be A1, A2, … etc. as shown
If the back surface of the block is in the far-field of the transducer, the incident and reflected waves will behave like attenuated spherical waves so we could express the voltage of these signals, v(t), in the form:
where the waveform shape is given by the g(t) function and is the average attenuation of the block (in Np/l)
Here is an example
A-scan we might see:
Notes: Here is an example response we might see. If the back surface of the block is sufficiently far from the transducer (i.e. in the “far field” of the transducer, which we define later) the reflected waves will look attenuated spherical waves so we can write the time domain response as shown.

## Slide 9
If we let gmax be the maximum amplitude of the g function then the amplitudes shown
are given by
If we take the ratio of the first two reflections we have
(1)
Notes: If we let gmax be the maximum of the g function then the amplitudes of these signal can all be written as shown. The ratio of the first two reflection amplitudes is then given by Eq. (1)

## Slide 10
Now
which gives
Notes: Assuming we measure this ratio we then can directly obtain an expression for the average attenuation. Note that because of the spherical wave spreading there is always a 6 dB decrease in the signal amplitude so that any material attenuation is seen in any changes greater than that 6 dB amount.

## Slide 11
Measurement of attenuation as a function of frequency
D1
D2
a
v0
material
to be measured
system function
acoustic/elastic transfer functions that describe the waves received from the front and back surface reflections
voltages received from front, back surface reflections
Notes: Now, consider how we might find a more detailed measurement of the attenuation as a function of frequency. We will again use a pulse-echo setup where we place both a transducer and a block of material (whose attenuation we want to measure) in a fluid and measure the front and back signals from the block [ Note: here we are only considering waves that have been reflected once from the front or back surfaces.]. We have seen previously that in the frequency domain, these reflected signals can be written as the product of a system function and an acoustic/elastic transfer function that describes the waves present in this setup.

## Slide 12
plane wave reflection, transmission coefficients
(normal incidence)
front surface transfer function
ideal transfer
function model
plane wave reflection coefficient
back surface transfer function
ideal transfer
function model
Notes: For ideal (non-attenuating) media we can actually model these acoustic/elastic transfer functions (see the next side) and then multiply them by the corresponding attenuation terms for both the water (whose attenuation is known) and the solid. Note that these models contain plane wave reflection and transmission coefficients at normal incidence.

## Slide 13
diffraction coefficient
In the back surface signal, the distance ¯ appearing
in the diffraction correction is:
D
Notes: The acoustic/elastic transfer functions also contain diffraction coefficient functions that are in terms of Bessel functions J0 and J1.

## Slide 14
measure
model
usually fit the attenuation to a simple polynomial
function of frequency over the bandwidth of the system
Here is an example of such a fitting
Notes: If we measure the ratio of the magnitude of these front and back surface response, we know from our models the ratio of the acoustic/elastic transfer functions, so we can write an expression for the frequency dependent attenuation we seek. Normally, we obtain this attenuation by fitting it to a simple polynomial function of frequency.

## Slide 15
Homework problems
D.1, S.2
Notes: Homework problem from Appendix D and a special problem.

## Slide 16
Remarks:
To measure attenuation, it is not necessary to measure
the system function (it cancels out).
Setup shown is for measurement of P-wave attenuation.
S-wave attenuation measurements must be done in
a different setup.
This approach is ad-hoc. Actual mechanisms of
attenuation are rather complex.
For high attenuation, wave speed as well as amplitude
is affected (material dispersion).
Notes: Here are some remarks on the method, which are self-explanatory.