## Slide 1
Acoustic/Elastic Transfer Function
Notes: The acoustic/elastic transfer function describes the waves propagating in the fluid and solid media present in an NDE test. This is not a function we can measure so we need to be able to model the function.

## Slide 2
Learning Objectives
Modeling the acoustic/elastic wave processes as
a transfer function
Blocked force concept
Special cases where the transfer function can be obtained analytically
Effects of material attenuation
Notes: Here, we will define the acoustic/elastic transfer function and discuss the concept of the blocked force. We will examine some cases where one can actually determine the acoustic/elastic transfer function analytically and show such an example where attenuation is also included.

## Slide 3
Acoustic/Elastic Transfer Function
All the complex wave propagation and scattering processes occurring in an ultrasonic measurement system can be characterized in terms of an acoustic/elastic transfer function
transmitted
force
received
"blocked" force
Notes: The acoustic/elastic transfer function is defined as the ratio of forces at the receiving and sending transducers. The force at the sending transducer is just the driving compressive force on the face of that transducer but at the receiver the force used is the blocked force. We will examine those forces in a pitch-catch immersion setup but we can consider a contact testing pitch-catch setup in a similar manner.

## Slide 4
pscatt
The Blocked Force on Reception
On reception the receiving transducer face moves and scattered waves are also generated
pinc
Notes: To see what the blocked force is consider a receiving transducer. Waves that are incident on that transducer will generate additional scattered waves.

## Slide 5
x
y
incident
wave
reflected
wave
rigid
boundary
The Blocked Force on Reception
If the incident waves are treated locally like plane waves and diffraction effects are ignored, we can consider the
interactions of the incident waves with the transducer face as those of plane wave with an infinite planar interface. Now, consider the case where the interface is held rigidly fixed:
The Blocked Force on Reception
Notes: Although the incident and scattered waves are likely not planar, we will treat the interaction of the waves with the receiving transducer as plane waves. Consider the case when the face of the transducer is modeled as a rigidly fixed surface.

## Slide 6
The Blocked Force on Reception
x
y
incident
wave
reflected
wave
rigid
boundary
In this case it can be shown that at the interface the blocked force is just double the force due to the incident wave only as if the transducer were absent, i.e
pinc
S
where
Notes: We will show that in this case the blocked force is just double that of the incident wave so we can compute the blocked force in this case only from the incident waves as if the transducer was absent.

## Slide 7
The Blocked Force on Reception
from vx = 0 at x = 0
x
(reflected pressure = inc. pressure)
Equation of motion:
or
Thus, also at x = 0
proof for normally incident waves
Notes: We have looked at plane wave interactions with an interface but now let us again examine the case where a plane wave is normally incident on a rigid ( motionless) surface. Placing harmonic waves into Newton’s law and using the boundary condition of no normal displacement, one finds the pressure amplitude of the reflected wave is just equal to that of the incident wave so that the total pressure is just double the incident pressure. The total force on the area of the receiving transducer face, therefore, will be just twice the incident force and this force is called the blocked force. Thus, in an ultrasonic setup if we can model the incident waves present at the receiving transducer coming from the sending transducer we can just double that force and use that result to calculate the acoustic/elastic transfer function.

## Slide 8
Acoustic/elastic processes model
For a number of calibration setups the acoustic/elastic
transfer function can be obtained explicitly:
front surface reflection
back surface reflection
reflection from flat-bottom hole
reflection from flat cylinder
Notes: In a number of setups we can model explicitly the acoustic/elastic transfer function. The ones shown here are all for pulse-echo setups.

## Slide 9
Acoustic Transfer Function
Example: the acoustic/elastic transfer function of two aligned
circular piston transducers of different radii can be found.
Notes: We can also obtain the acoustic/elastic transfer function in this pitch/catch setup where two circular transducers are aligned along their central axes in a water bath. The explicit function is shown here in terms of an integral.

## Slide 10
Special Cases
a = b :
Acoustic Transfer Function
At the high frequencies found for most NDE transducers
the above integral can be evaluated approximately to yield:
Notes: Here we show the special case where the two transducers are of the same size. In this case, at the high frequencies found in most ultrasonic NDE transducers the integral can be approximated in terms of Bessel functions to yield an explicit expression for the acoustic/elastic transfer function.

## Slide 11
a >> b :
a << b :
D >> a, b :
Acoustic Transfer Function
Other special cases:
Notes: Here are also some special cases where we can obtain analytical expressions for the transfer function.

## Slide 12
Acoustic Transfer Function
Attenuation of ultrasound in the fluid can be added
to this model:
a(w) … attenuation coefficient
For water
1/mm
f… frequency in MHz
D … distance traveled
Notes: All the results we have shown for the acoustic/elastic transfer functions were for an ideal (i.e. non-attenuating) fluid media. However, as we showed previously we can easily include an attenuation factor to account for losses, and for water, in particular, we can describe the attenuation coefficient.

## Slide 13
Example acoustic transfer function (including fluid
attenuation effects)
Acoustic Transfer Function
D = 444 mm
a = 3.175 mm
0
5
10
15
20
0
0.05
0.1
0.15
0.2
0.25
0.3
0.35
0.4
0
5
10
15
20
-90
-85
-80
-75
-70
-65
-60
-55
-50
-45
-40
Frequency (MHz)
Phase (Deg)
Amplitude
amplitude
phase
Notes: Here is an example calculation for the acoustic/elastic transfer functions for a pair of NDE immersion transducers where attenuation of the water is included in the calculations.

## Slide 14
Acoustic Transfer Function
Goldstein, A., Gandhi, D.R., and W.D. O’Brien,” Diffraction
effects in hydrophone measurements,” IEEE Trans. Ultrasonics,
Ferroelectrics, and Freq. Control, 45, 972-979, 1998.
Notes: Here is a reference on some of the issues discussed here. There are many others as well.