## Slide 1
Flaw Scattering Models
Notes: Having examined the waves generated by transducers we now need to consider the scattered waves generated when an incident wave strikes a flaw.

## Slide 2
Learning Objectives
Far-field scattering amplitude
Kirchhoff approximation
Born approximation
Separation of Variables
Examples of scattering of simple shapes
(spherical pore, flat crack, side-drilled hole)
Notes: We will see that the waves scattered from a flaw can be described in terms of a far field scattering amplitude and examine three different methods for modeling those scattered waves. We will examine scattering for some of the simple shapes commonly used as reference “flaws”.

## Slide 3
Flaw Scattering
rs
es
xs
y
n
flaw
ei
p0
Incident plane
wave
p0 … pressure
amplitude
Fluid Model
At many wavelengths away from the flaw the
scattered waves are spherical waves
scattered pressure
A is called the plane wave far-field scattering amplitude
Notes: In most NDE inspections the flaw being examined will be located at many wavelengths from the receiving transducer. In that case the flaw acts like a point source having a complicated radiation pattern, i.e. it radiates a spherical wave with an amplitude coefficient that is called the far field scattering amplitude. Shown is the case for a scatterer in a fluid where the incident wave is a plane wave and A is the plane wave far field scattering amplitude. A is a function of both the incident and scattering directions of the waves as well as the frequency but we will typically show the unit vectors ei and es that define the incident and scattered directions in the arguments of A but not the frequency. Note that A has the dimensions of a length.

## Slide 4
plane wave far field scattering amplitude of the flaw
Flaw Scattering
rs
es
xs
y
n
flaw
ei
p0
Incident plane
wave
p0 … pressure
amplitude
Fluid Model
Notes: In the fluid case just described we can actually write down an integral expression for the plane wave far field scattering amplitude in terms of the normalized pressure and its normal derivative (the normal derivative of the pressure is just proportional to the normal velocity, as shown), where the integral is taken over the surface of the flaw. The unit vector es here is a unit vector in the scattering direction being examined.

## Slide 5
Flaw Scattering
To obtain the far field scattering amplitude, we need to know the
pressure and velocity on the surface of the flaw due to the incident
and scattered waves
These quantities can be found by solving a flaw scattering
boundary value problem.
Notes: To describe the scattering amplitude we need both the pressure and its normal derivative (or, equivalently, the normal velocity) on the flaw surface which can be found by solving a boundary value problem. To avoid having to go into that detail we can try to use approximations to obtain these surface fields. Shortly, we will examine such approximations

## Slide 6
Flaw Scattering
Elastic Solid
rs
n
flaw
U0
U0 … displacement
amplitude for wave
of type b (b = P,S) in
problem (1)
Scattered wave of
type a (a = P,S)
scattered displacement
from a flaw
P-wave
S-wave
Notes: If we look at flaw scattering in an elastic solid we see much the same picture as in the fluid case but now at many wavelengths the scattered waves are both spherical P-waves and S-waves and the scattering amplitudes are vectors since they must represent a vector field such as the scattered displacements. The incident waves themselves also can be either P-waves or S-waves.

## Slide 7
Flaw Scattering
Vector scattering amplitude for a scattered wave of
type a due to a plane wave of unit displacement
amplitude and type b
elastic
constants
displacements and displacement
gradients
Notes: We can express both the scattered P- and S-waves in terms of a vector function f which can be represented as an integral over the surface of the flaw of both the displacements and the displacement gradients. These surface fields again can be found by solving a particular boundary value problem or through approximations.

## Slide 8
Flaw Scattering
The received voltage in some measurement models is related to a specific component of the vector scattering amplitude given by
3-D scattering amplitude
polarization vector of an incident wave from receiving transducer (to be discussed shortly)
Notes: The received voltage in a measurement is a scalar quantity so that if it is related to the scattering amplitude, it must involve a specific component of the vector scattering amplitude, which we call A. We will see shortly that this scalar component is obtained by taking the dot product of the vector scattering amplitude with a polarization vector associated with the receiving transducer when it acts as a transmitter. We will describe this component later.

## Slide 9
Flaw Scattering
A(w) can be obtained from:
Numerical methods
Separation of variables
Boundary Elements (BEM)
Finite Elements (FEM)
Method of Optimal Truncation (MOOT)
T-matrix
Approximate Methods
Kirchhoff Approximation
Born Approximation
or A(w) can be found experimentally through
deconvolution:
measure
model, measure
Notes: If we solve a boundary value problem whose solution gives the surface fields needed to define the scattering amplitude, that solution is normally obtained with numerical methods, a number of which are shown above. Here, we will discuss only one of those methods, the method of separation of variables. Alternatively, we can use approximate methods. We will talk about two of those approximations – the Kirchhoff approximation and the Born Approximation.
There is also an experimental way to obtain the scattering amplitude. If we measure the voltage response of the flaw in a setup where we can model or measure all of the other parts of the system, then we can obtain the scattering amplitude through deconvolution, which is normally done, as shown above, with a Wiener filter.

## Slide 10
Flaw Scattering
Kirchhoff Approximation for a Volumetric Flaw
on the "lit" surface: fields are those from plane waves
interacting with a plane surface
on the rest of the surface the fields are assumed to be zero
S
l
i
t
D
n
i
n
c
i
d
e
n
t
w
a
v
e
r
e
f
l
e
c
t
e
d
w
a
v
e(s)
O
x
x
s
e
i
e
r
t
a
n
g
e
n
t
p
l
a
n
e
P
Notes: First, consider the Kirchhoff approximation. This is an approximation suitable for high frequencies where the fields on the portion of the surface where the waves directly strike the flaw (called the “lit” surface) are obtained by calculating the interaction of the incident wave (taken to be a plane wave) with a planar surface whose unit normal coincides with the normal to the surface. This plane wave interaction problem can be solved exactly so we obtain the surface fields over the entire lit surface. Over the remaining of the surface the fields are assumed to be identically zero.

## Slide 11
Flaw Scattering
It has been recently shown that the pulse-echo scattering amplitude response, A(w), for a stress-free flaw (void or crack) in an elastic solid is identical to the scalar (fluid) scattering amplitude:
Notes: Although in general the scattered response in an elastic solid is quite different from that of a flaw in a fluid, it has been shown that for a stress-free flaw (crack or void) the pulse-echo response for the scattering amplitude is the same for both the fluid and elastic problems yielding an explicit integral over the lit surface that can be evaluated. This allows us to use the simple fluid model even in the elastic wave case.

## Slide 12
Flaw Scattering-Spherical Void
For the pulse-echo response of a spherical
void of radius a, fluid model
0
5
10
15
20
25
30
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
frequency, MHz
|A(w)|
a = 1 mm
c = 5900m/s
2a
Notes: Performing the scattering amplitude integral exactly for a spherical void, we can plot the magnitude of the pulse-echo scattering amplitude response as a function of the frequency.

## Slide 13
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
frequency, MHz
2|A|/a
Comparison with Kirchhoff solution with
exact separation of variables solution for the P-P scattering
amplitude of a void in an elastic solid (pulse-echo)
leading edge
response
"creeping" wave
exact solution (solid line)
Kirchhoff solution
(dotted line)
Flaw Scattering-Spherical Void
Notes: We can also calculate the P-P pulse echo scattering amplitude of the spherical void in an elastic solid numerically (i.e. without approximation) and compare it with the Kirchhoff approximation. We see the two responses have many similarities in terms of their general amplitudes but the oscillations in the responses are different. This difference arises from the fact that the oscillations in the Kirchhoff approximation come from the interference of a large reflection from a point on the surface where the wave first strikes the void (called the leading edge response) with the reflections from the remainder of the lit surface. In contrast, the exact separation of variables solution oscillations come from an interference of the leading edge response with a so-called creeping wave that travels around the flaw and returns in a direction opposite to the incident wave direction in the pulse-echo setup. The leading edge response is contained in both the separation of variables and Kirchhoff approximation solutions but the creeping wave is not predicted by the Kirchhoff approximation.

## Slide 14
Inverting the scattering amplitude (fluid model) predicted
by the Kirchhoff approximation into the
time domain
A(t)
t
leading edge
response
"lit" surface
response
Flaw Scattering-Spherical Void
Notes: If we invert the Kirchhoff approximation solution into the time domain with an inverse Fourier transform, we see a delta function leading edge response followed by a box-like function over the lit surface (i.e. the front half of the sphere).

## Slide 15
Exact solution
for a void in an
elastic solid (time
domain)
vs the Kirchhoff
approximation solution
time,
m
sec
-
2
0
2
4
6
8
10
-
1.5
-
1
-
0.5
0
0.5
1
1.5
2
2.5
time,
m
sec
-
2
0
2
4
6
8
10
-
1.5
-
1
-
0.5
0
0.5
1
1.5
2
2.5
creeping wave
Flaw Scattering-Spherical Void
Notes: In contrast, we see here the separation of variables solution (plotted in blue) where the leading edge delta function has been removed since it is identical with the delta function obtained from the Kirchhoff approximation. By removing the delta function the remaining waves frequency content is small at high frequencies so we easily perform an inverse FFT to obtain the time-domain waveforms. In addition to the response over the lit surface (which is not a constant) we see a later arriving wave which is the creeping wave. The Kirchhoff approximation is shown as the dotted line response, which includes (symbolically) the delta function .

## Slide 16
Although the Kirchhoff approximation is formally a high frequency approximation ( ka >>1), numerical tests have shown it capable of producing good agreement (<1 dB difference) for the peak-to-peak time domain response of the spherical void down to ka =1 provided the bandwidth is sufficient
bandwidth, %
ka
10
20
30
40
50
60
70
80
90
0.5
1
1.5
2
2.5
3
3.5
4
4.5
5
white: differences <1 dB
gray: >1 dB but < 1.5 dB
black: > 1.5 dB
Flaw Scattering-Spherical Void
Notes: Comparisons of the Kirchhoff approximation with the separation of variables solution show that the Kirchhoff approximation, while it is formally a high frequency approximation (ka >>1) ,where k is the wave number and a is the flaw radius, actually models the amplitude of the pulse-echo signal quite well down to ka =1 provided the bandwidth is sufficiently large

## Slide 17
Flaw Scattering-Inclusion
Leading Edge Response - General Convex Inclusion
(scattered mode same as incident mode)
High frequency, stationary phase approximation
Plane wave reflection coefficient
Gaussian curvature of flaw surface at
stationary phase point
n
d
e
s
e
i
S
lit
tangent plane
q
i
a
a
x
s
stat
e
s
Notes: The leading edge response is a key part of the Kirchhoff approximation response and in fact at high frequencies is part of the exact response of flaws that is often the dominant response. Shown is the leading edge pitch-catch, same mode response of a general complex-shaped convex flaw (void or inclusion). The leading edge response amplitude depends on the plane wave reflection coefficient and the Gaussian curvature of the flaw at a point on the surface called the specular point where the unit normal to the surface and the incident and scattered wave directions are related through Snell’s law. For cases where there are multiple specular points then all such points contribute to the response.

## Slide 18
Flaw Scattering-Inclusion
In the time domain
Leading Edge Response - General Convex Inclusion
(scattered mode same as incident mode)
n
d
e
s
e
i
S
lit
tangent plane
q
i
a
a
x
s
stat
e
s
Notes: If we transform the leading edge response into the time domain, we see a delta function.

## Slide 19
Flaw Scattering-Crack
Kirchhoff Approximation – Flat Elliptical Cracks
Notes: We can also obtain some solutions for cracks in the Kirchhoff approximation. Here is the pitch-catch response of a flat elliptical crack (fluid model) which involves a Bessel function, J1.

## Slide 20
General pitch-catch crack response-circular crack
The magnitude of the P-wave pulse-echo far-field scattering amplitude versus frequency for a 1 mm radius circular crack in steel
with an angle of incidence of from the crack normal.
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
frequency, MHz
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
frequency, MHz
Flaw Scattering-Crack
Notes: If we plot the pitch-catch response in the frequency domain we see a series of decreasing peaks and nulls in the response. These oscillations, we will see, arise because of the existence of so-called flash-points in the time domain response.

## Slide 21
Comparison of the Kirchoff approximation and MOOT for a 0.381 mm radius circular crack at an incident angle of 45 degrees (pulse-echo)
0
5
10
15
20
25
0
0.05
0.1
0.15
0.2
0.25
frequency, MHz
amplitude
KIR
MOOT
inc = 45
Flaw Scattering-Crack
Notes: There is a more exact numerical approach to solving scattering problems called MOOT (for the Method Of Optimal Truncation) that can be compared with the Kirchhoff approximation result. The MOOT results show the overall behavior of the Kirchhoff approximation result but contain additional oscillations that are due to the interference of other waves that are present besides the flash points.

## Slide 22
When eq is parallel to the crack normal, n :
Special case - pulse echo:
ei
es
n
eq
ei
es
n
The magnitude of the P-wave pulse-echo far-field scattering amplitude versus frequency for a 1 mm
radius circular crack in steel at normal incidence.
0
5
10
15
20
25
30
0
2
4
6
8
10
12
14
16
frequency, MHz
0
5
10
15
20
25
30
0
2
4
6
8
10
12
14
16
frequency, MHz
Flaw Scattering-Crack
Notes: In certain cases such as normal incidence (for pulse-echo) the Kirchhoff response is quite different, becoming a linearly increasing function of frequency. We will see this arises because the time-domain response becomes a doublet (derivative of a delta function) in the time domain in this case.

## Slide 23
Comparison of the Kirchoff approximation and MOOT for a 0.381 mm radius crack at normal incidence (pulse-echo)
0
5
10
15
20
25
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
frequency, MHz
amplitude
KIR
MOOT
inc=0
numerical errors in MOOT
Flaw Scattering-Crack
Notes: A MOOT solution also shows a general linearly increasing behavior but with some small oscillations that decay at higher frequencies. However, a more careful numerical solution revealed that the oscillations actually continue at these higher frequencies. This MOOT solution did not keep a sufficient number of terms in this solution.

## Slide 24
Inverting these results into the time domain
flash points
Example: pulse-echo
t
Flaw Scattering-Crack
Notes: If we invert the crack Kirchhoff response into the time domain we find an antisymmetric pair of pulses called flash points, that arise in pulse-echo, for example, when the incident wave first touched the flaw edge and last touches the edge.

## Slide 25
At normal incidence, for pulse-echo
A
(
e
;
e
)
i
s
t
Flaw Scattering-Crack
Notes: In the pulse-echo response at normal incidence, we obtain instead a doublet response (derivative of a delta function) in the time domain that has the linearly increasing frequency response we saw previously.

## Slide 26
A planar crack is a very “specular” reflector
q
0
10
20
30
40
50
60
70
80
90
0
0.5
1
1.5
2
2.5
3
angle, degrees
Flaw Scattering-Crack
Notes: At a given frequency the crack behaves as a very specular reflector, i.e. its response is large in pulse-echo, only when the incident wave direction is normal to the face of the crack. However, real crack responses come from a range of frequencies so that we will show through some numerical studies that this behavior at a single frequency is misleading and the Kirchhoff approximation can often be used at a wide range of angles.

## Slide 27
white: differences <1 dB
gray: >1 dB but < 1.5 dB
black: > 1.5 dB
Although the Kirchhoff approximation is formally a high frequency approximation ( ka >>1), numerical tests have shown it capable of producing good agreement (<1 dB difference) for the peak-to-peak time domain response of a circular crack at normal incidence down to ka =1.5 provided the bandwidth is sufficient
bandwidth, %
10
20
30
40
50
60
70
80
90
0.5
1
1.5
2
2.5
3
3.5
4
4.5
5
ka
Flaw Scattering-Crack
Notes: For example, numerical studies have shown that the peak-to-peak amplitude of the crack response is in good agreement with more exact solution to frequencies as low as ka = 1.5 provided the bandwidth is sufficient.

## Slide 28
Comparison of synthesized waveforms scattered from a 0.381 mm radius crack using the Kirchhoff approximation and MOOT using frequencies from 0-25 MHz approximately (pulse echo)
0
5
10
15
20
25
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1
amplitude
frequency, MHz
Flaw Scattering-Crack
Notes: We will compare the Kirchhoff and MOOT ( considered here to be the “exact” solution) results over a wide band of frequencies and invert these frequency domain results into the time domain so we can examine the scattered waveforms. The MOOT results are left unaltered from zero to 15 MHz, then are smoothly tapered to zero at 25 MHz with the filter shown. This filter generates a wide band response with little ringing in the time domain that can be compared with the Kirchhoff results.

## Slide 29
0-15 degrees from crack normal
-20
-15
-10
-5
0
5
10
15
20
KIR
MOOT
0
5
10
15
Flaw Scattering-Crack
Notes: This shows the Kirchhoff (blue) and MOOT pulse-echo results of a circular crack for angles of 0, 5, 10, and 15 degrees from the normal, respectively (all plotted on the same axis). Generally, we only see a bandlimited doublet response, which is predicted to have the same form for both theories, although the MOOT also contains some small later arriving waves.

## Slide 30
20-35 degrees from crack normal
Flaw Scattering-Crack
Notes: This comparison is for angles of 20, 25 30 and 35 degrees from the crack normal, where we see the flash points forming in the response but where now MOOT also predicts some larger later arriving waves.

## Slide 31
40-55 degrees from crack normal
Flaw Scattering-Crack
Notes: This continues the study for angles of 40, 45, 50, and 55 degrees from the normal. It is seen the flash points remain the dominant part of the response and that the two theories agree well for those flashpoints (although the second flashpoint is becoming somewhat smaller in the MOOT response from that of the completely antisymmetrical Kirchhoff result) , but that by 55 degrees the later arriving waves have became as large as the first flashpoint.

## Slide 32
60-70 degrees from crack normal
Flaw Scattering-Crack
Notes: At 60, 65 and 75 degrees the first flashpoint responses of the two theories still agree quite well but the second flashpoint of the MOOT result is now much smaller than the first flashpoint and the later arriving waves are now larger than the flashpoint responses.

## Slide 33
75-85 degrees from crack normal
Flaw Scattering-Crack
Notes: At the extreme angles of 75, 80, and 85 degrees the general behavior seen on the previous slide continues. If we compare the amplitudes here with the normal incidence case we see the amplitudes here are much smaller, so the crack is indeed rather specular in nature but the Kirchhoff approximation remains valid over a wide range of angles and is not limited in validity to near normal incidence.

## Slide 34
Comparison of peak-to-peak values of MOOT and Kirchhoff versus angle of incidence for the 0.381mm radius crack (pulse-echo)
The arrow shows where agreement is within 1 dB
Flaw Scattering-Crack
Notes: This slide shows that the peak-to-peak amplitudes of the Kirchhoff and MOOT solutions agree, for these 0-25 MHz bandwidth responses out to about 60 degrees.

## Slide 35
Now consider the scattering amplitude with narrow band Gaussian window
The central frequency is 10 MHz, and the bandwidth is 1 MHz
Radius of the crack a = 0.381mm
0
5
10
15
20
25
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1
frequency, MHz
amplitude
Flaw Scattering-Crack
Notes: In contrast, we now band limit the frequency domain responses to a very narrow bandwidth, as shown.

## Slide 36
the range of angles where the agreement is good is significantly reduced
Flaw Scattering-Crack
Notes: In this narrow bandwidth case the range of angles of agreement is substantially smaller.

## Slide 37
Now consider the scattering amplitude with wider band Gaussian
window
The central frequency is 10 MHz, and the bandwidth is 6 MHz
Radius of the crack a = 0.381mm
0
5
10
15
20
25
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1
frequency, MHz
amplitude
Flaw Scattering-Crack
Notes: Now, expand the bandwidth a bit.

## Slide 38
The range of excellent agreement now is back to angles as great as 45 degrees or more
Flaw Scattering-Crack
Notes: We see the range of angles with good agreement is now substantially larger.

## Slide 39
Flaw Scattering
10
20
30
40
50
60
70
80
90
10
15
20
25
30
35
40
45
50
55
60
bandwidth, %
max. incident angle, degrees
Maximum incident angle where the peak-to-peak time domain agreement between the Kirchhoff approximation and the exact solution for a circular crack is less than 1 dB for ka =5.0 (other ka values shown same trend).
Flaw Scattering-Crack
Notes: This curve summarizes the effects of bandwidth on the maximum angle at which the Kirchhoff and MOOT results are in good agreement. We see that bandwidth indeed plays a key role in where the Kirchhoff approximation is valid. This is important since in practice the flash point signals are often used in NDE inspections for important tasks such as sizing a crack.

## Slide 40
Kirchhoff approximation for pulse-echo scattering of a side-drilled hole (incident direction in plane perpendicular to the hole axis)
L
2b
Bessel function
Struve function
Flaw Scattering-SDH
Notes: In addition to spherical voids and circular or elliptical flat cracks, we can get an explicit result for the pulse-echo scattering amplitude of a side-drilled hole (for either incident/scattered P-waves or S-waves). This type of scatterer is often used in calibration studies. We see the response is in terms of a Bessel function, J1 , and a Struve function, S1 .

## Slide 41
Flaw Scattering-SDH
Comparison with exact 2-D separation of variables
solution for P-waves (pulse-echo)
The three-dimensional normalized pulse-echo P-wave scattering amplitude versus normalized wave number for a side drilled hole in the Kirchhoff approximation (solid line) and from the exact two-dimensional separation of variables solution (dashed line).
0
2
4
6
8
10
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
0
2
4
6
8
10
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
Notes: If we compare the Kirchhoff response (solid line) with an “exact” separation of variables solution (dashed line) for P-waves we see good agreement but as in other cases there are more oscillations in the exact result, likely coming from the interference of waves that are not included in the Kirchhoff approximation.

## Slide 42
Flaw Scattering-SDH
Comparison with exact 2-D separation of variables
solution for S-waves (pulse-echo_)
The three-dimensional normalized pulse-echo SV-wave scattering amplitude versus normalized wave number for a side drilled hole in the Kirchhoff approximation (solid line) and from the exact two-dimensional separation of variables solution (dashed line).
0
2
4
6
8
10
0
0.2
0.4
0.6
0.8
1
1.1
0
2
4
6
8
10
0
0.2
0.4
0.6
0.8
1
1.1
Notes: In contrast, for S-waves incident on the side-drilled hole there are more severe oscillations in the separation of variables solution.

## Slide 43
Flaw Scattering
Kirchhoff approximation - Summary
For volumetric flaws -the Kirchhoff approximation properly models the leading edge signal as long as ka >1 approximately but does not model other waves (creeping waves, etc.)
For cracks – the Kirchhoff approximation models the flash point signals properly in pulse-echo as long as ka > 1 approximately and the incident angle is less than about 50 degrees for wide band responses. For narrow band responses this angle is considerably reduced to as little as 15-20 degrees.
Notes: In summary, the Kirchhoff approximation , while it does not capture all the aspects of the flaw response, it does model very well the leading edge signals of volumetric flaws and the flashpoint signals of cracks and those signals are often the dominant signals seen and used in NDE tests. In fact, we have shown that it is the leading edge responses of volumetric flaws (and the flashpoints, for cracks) that are primarily responsible for generating the flaw images seen in popular flaw imaging methods such as SAFT (synthetic aperture focusing technique) and Full-Matrix Capture imaging.

## Slide 44
Flaw Scattering -Inclusion
The Born approximation assumes that the material of an inclusion differs little from the host material so that to first order the incident wave passes through the inclusion unchanged (weak scattering, low frequency approximation)
incident wave
einc
The Born Approximation
Notes: Another approximation that has been used is the Born approximation that assumes the flaw is nearly the same as the host material so that to first order the incident wave is unchanged as it passes through the flaw. It is a weak scattering, low frequency approximation.

## Slide 45
The Born approximation generally is developed from a volume integral expression for the scattering amplitude
density difference
difference in elastic constants
fields in the flaw replaced by incident fields
Flaw Scattering -Inclusion
Notes: The Born approximation is based on a volume integral representation of the scattering amplitude and simply replaces the fields in that volume integral by the incident wave fields, leading to an explicit representation for the scattering amplitude.

## Slide 46
For a spherical inclusion in pulse-echo
spherical Bessel function
where
relative density
difference
relative wave speed
difference
Flaw Scattering -Inclusion
Notes: For the pulse-echo response of a spherical inclusion the response is in terms of a spherical Bessel function, j1 .

## Slide 47
Corresponding time domain impulse response for a spherical inclusion (pulse-echo)
front surface
response
back surface
response
Flaw Scattering -Inclusion
Notes: If one inverts the spherical inclusion response into the time domain one finds delta function front and back surface responses and a constant response throughout the flaw in between the front and back surfaces.

## Slide 48
Comparison with "exact" separation of variables solution
for the pulse-echo response of a spherical inclusion by synthesizing a time-domain response from frequencies ranging from 0-20 MHz approximately for a 1 mm radius inclusion (10 % differences in properties)
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where the density
and compressional wave speed are both ten percent higher than the host steel. Solid line:
Born approximation, dashed line: separation of variables solution.
-
1
-
0.5
0
0.5
1
-
0.5
0
0.5
1
1.5
amplitude
time,
m
sec
-
1
-
0.5
0
0.5
1
-
0.5
0
0.5
1
1.5
amplitude
time,
m
sec
Flaw Scattering -Inclusion
Notes: Here is a comparison of the Born approximation with an “exact” separation of variables solution for a weakly scattering spherical inclusion, showing the leading delta function responses are nearly identical and the back surface responses are similar but somewhat displaced. In addition, there are other responses of later arriving waves in the “exact” solution not predicted by the Born approximation.

## Slide 49
Comparison with "exact" separation of variables solution
for the pulse-echo response of a spherical inclusion by synthesizing a time-domain response from frequencies ranging from 0-20 MHz approximately for a 1 mm radius inclusion (50 % differences in properties)
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where the density
and compressional wave speed are both fifty percent higher than the host steel.Solid line: Born approximation,
dashed line: separation of variables solution.
amplitude
errors
time of arrival errors
-
1
-
0.5
0
0.5
1
-
4
-
2
0
2
4
6
8
amplitude
time,
m
sec
-
1
-
0.5
0
0.5
1
-
4
-
2
0
2
4
6
8
amplitude
time,
m
sec
Flaw Scattering -Inclusion
Notes: For a spherical inclusion with properties significantly different from that of the host the front surface signals are very similar but the back surface responses are significantly different in amplitude and time of arrival and there are again other significant waves present not predicted by the Born approximation.

## Slide 50
Doubly Distorted Born Approximation
replace wave speeds of host material by that of the flaw in the Born approximation
for the pulse-echo response of a spherical
inclusion
where
Flaw Scattering -Inclusion
Notes: Since most real flaws found in NDE inspections are not weak scatterers, it would be nice to be able to “fix” the time of arrival and amplitude errors we have just seen. An ad-hoc fix called the doubly distorted Born approximation was developed that simply replaces the wave speed in the F function and the spherical Bessel function by the flaw wave speed rather than the surrounding host wave speed found in the Born approximation. This makes sense since the wave propagating in the flaw travels at the flaw wave speed not that of the host.

## Slide 51
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where the density and compressional wave speed are both fifty percent higher than the host steel. Solid line: Doubly Distorted Born approximation, dashed line: separation of variables solution.
Front surface amplitude response is improved, and relative time of arrival of back surface response is correct, but there is an error in absolute time of arrivals (50% differences in properties)
-
1
-
0.5
0
0.5
1
-
4
-
2
0
2
4
6
8
amplitude
time,
m
sec
-
1
-
0.5
0
0.5
1
-
4
-
2
0
2
4
6
8
amplitude
time,
m
sec
Flaw Scattering -Inclusion
Notes: Comparisons of the doubly distorted Born approximation with the separation of variables solution for a strongly scattering spherical inclusion shows that the doubly distorted Born approximation does now get the time separation between the front and back signals correct but the amplitudes of both signals are still different and the front and back signals do not have the correct times of arrival.

## Slide 52
Why is the front surface response amplitude improved by the Doubly Distorted Born Approximation ?
Answer: because
(plane wave reflection coefficient)
1
1.2
1.4
1.6
1.8
2
2.2
2.4
2.6
2.8
3
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
1
1.2
1.4
1.6
1.8
2
2.2
2.4
2.6
2.8
3
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
F
R12
Flaw Scattering -Inclusion
Notes: The amplitude of the front response in the doubly distorted Born approximation is closer to the exact solution than the ordinary Born approximation. The modified F function we see is closer to the exact plane wave reflection coefficient for the flaw so it seems likely that better agreement is the reason for the improvement.

## Slide 53
This suggests we apply a phase correction to the doubly distorted Born approximation and replace by
resulting in the modified Born approximation (MBA)
for the pulse-echo response of a spherical
inclusion
phase correction
Flaw Scattering -Inclusion
Notes: Thus, instead of using the doubly distorted Born approximation, it makes sense instead to replace the F function by the plane wave reflection coefficient and add a phase term to account for the time of arrival errors. This simple modification we have called the modified Born approximation.

## Slide 54
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where the density and compressional wave
speed are both fifty percent higher than the host steel.Solid line: MBA approximation, dashed line: separation of variables solution.
The MBA
(50 % differences in properties)
-
1
-
0.5
0
0.5
1
-
2
-
1
0
1
2
3
4
5
6
amplitude
time,
m
sec
-
1
-
0.5
0
0.5
1
-
2
-
1
0
1
2
3
4
5
6
amplitude
time,
m
sec
Flaw Scattering -Inclusion
Notes: Here is now a comparison of the modified Born approximation with the separation of variables solution for a strongly scattering inclusion. We see the font surface responses now match almost perfectly and the time of arrivals of both the front and back surfaces are now correct also. The amplitudes of the back surface responses are still different as the Born approximation always assumes the front and back surface responses are identical and this is simply not the case in practice except in the weakly scattering limit.

## Slide 55
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where
the density and compressional wave speed are both one hundred percent higher than the host steel.
Solid line: MBA approximation, dashed line: separation of variables solution.
The MBA
(100 % differences in properties)
-
1.5
-
1
-
0.5
0
0.5
1
1.5
2
-
10
-
5
0
5
10
15
20
amplitude
time,
m
sec
-
1.5
-
1
-
0.5
0
0.5
1
1.5
2
-
10
-
5
0
5
10
15
20
amplitude
time,
m
sec
Flaw Scattering -Inclusion
Notes: Even at 100 per cent differences between the flaw and host properties the modified Born approximation continues to get at least the front surface signal correct. Note the many late arriving signals in the exact response. There are many other waves present that travel both in the inclusion and around it that are not accounted by the Born approximation.

## Slide 56
The sphere and the cylinder are the only two geometries
where we can obtain exact separation of variables solutions for elastic wave scattering problems. These are commonly used as "exact" solutions to test more approximate theories and numerical methods.
The Method of Separation of Variables
Flaw Scattering
Notes: The method of separation of variables gives us an “exact” method to calculate scattering properties of spherical and cylindrical flaws so it is an important tool for making comparisons with approximate theories, as we have shown.

## Slide 57
Flaw Scattering-Void
Example 1: pulse-echo P-wave scattering of a spherical void
Notes: The separation of variables solution for the pulse-echo P-wave response for a spherical void is shown here. It involves an infinite sum of special function terms which must be truncated for numerical purposes. Generally more terms are needed at the higher frequencies. It is not difficult to calculate on the order of 100 terms in the sum and this typically is enough to cover the frequencies found in most NDE tests.

## Slide 58
Flaw Scattering-Void
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
frequency, MHz
2|A| / b
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
frequency, MHz
2|A| / b
The normalized P-wave pulse-echo scattering amplitude 2A/b
for a spherical void of radius b.
Notes: Here is the pulse echo response of a spherical void as calculated with the method of separation of variables. It looks similar to the Kirchhoff approximation response. At high frequencies the amplitudes agree but the oscillations are different, especially at low frequencies.

## Slide 59
Flaw Scattering-Void
Using this separation of variables solutions at many frequencies to synthesize a P-wave impulse time domain solution (pulse-echo)
The time-domain pulse-echo P-wave response of a 0.5 mm radius spherical void in steel ( cp = 5900 m/s, cs = 3200 m/sec)
obtained by applying a low-pass cosine-squared windowing filter between 10 and 20 MHz to the separation
of variables solution and then inverting the result into the time domain with the inverse Fourier transform.
time,
m
sec
amplitude
-
1
-
0.5
0
0.5
1
1.5
-
12
-
8
-
4
0
6
time,
m
sec
amplitude
-
1
-
0.5
0
0.5
1
1.5
-
12
-
8
-
4
0
6
Notes: If we use that frequency domain response and calculate the time domain response we see the leading edge response and a response over the lit surface which is not constant as found in the Kirchhoff approximation. There also is a later arriving creeping wave which has traveled around the sphere and is not predicted by The Kirchhoff approximation.

## Slide 60
Flaw Scattering-Void
Example 2: pulse-echo SV-wave scattering of a spherical void
Notes: Here is the separation of variables pulse-echo solution for an SV-wave incident on a spherical void.

## Slide 61
Flaw Scattering-Void
The SV-wave pulse-echo scattering amplitude
The magnitude of the pulse-echo SV-wave response, , versus frequency for a 0.5 mm radius spherical void in steel
( cp = 5900 m/s, cs = 3200 m/sec) as calculated by the method of separation of variables
0
2
4
6
8
10
12
14
16
18
20
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
frequency, MHz
amplitude
0
2
4
6
8
10
12
14
16
18
20
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
frequency, MHz
amplitude
Notes: In the frequency domain there now are considerably more oscillations present, suggesting the presence of large, later arriving waves.

## Slide 62
Flaw Scattering-Void
Using this separation of variables solutions at many frequencies to synthesize an SV-wave impulse time domain solution (pulse-echo)
The time domain pulse-echo SV-wave response for the same void considered in the P-wave case by applying a low-pass cosine-squared windowing filter between 10 and 20 MHz to the separation of variables solution and then inverting the result into the time domain with the inverse Fourier transform.
-
1
-
0.5
0
0.5
1
1.5
-
12
-
8
-
4
0
6
time,
m
sec
amplitude
-
1
-
0.5
0
0.5
1
1.5
-
12
-
8
-
4
0
6
time,
m
sec
amplitude
Notes: Transforming the response into the time domain we see the leading edge response again but now there is a very strong later arriving creeping wave.

## Slide 63
Flaw Scattering- SDH
Example 3: pulse-echo P-wave scattering of a cylindrical void
Notes: We can also write down a separation of variables solution for a P-wave incident on a cylindrical void. This is a 2-D scatterer where we can define its scattering in terms of a 3-D scattering amplitude or a 2-D scattering amplitude, which are simply related.

## Slide 64
Flaw Scattering-SDH
Recall, the scattering amplitude for the pulse-echo P-wave case was:
0
2
4
6
8
10
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
Notes: This gives the response in the frequency domain we saw previously and which was generally in good agreement with the Kirchhoff approximation.

## Slide 65
Flaw Scattering- SDH
Using this separation of variables solutions at many frequencies to synthesize a P-wave impulse time domain solution (pulse-echo)
The time-domain pulse-echo P-wave response of a 0.5 mm radius cylindrical void in steel (cp = 5900 m/s, cs = 3200 m/sec) obtained by
applying a low-pass cosine-squared windowing filter between 10 and 20 MHz to the separation of variables solution and then inverting the
result into the time domain with the inverse Fourier transform.
-
1
-
0.5
0
0.5
1
1.5
-
30
-
20
-
10
0
10
20
30
time,
m
sec
amplitude
creeping wave
-
1
-
0.5
0
0.5
1
1.5
-
30
-
20
-
10
0
10
20
30
time,
m
sec
amplitude
creeping wave
Notes: If we invert the result into the time domain we see the leading edge response and a weak creeping wave.

## Slide 66
Flaw Scattering - SDH
Example 4: pulse-echo SV-wave scattering of a cylindrical void
Notes: If instead we examine the pulse-echo SV-wave response of the cylindrical void we also can write down the separation of variables solution.

## Slide 67
Flaw Scattering -SDH
Again, the scattering amplitude for the pulse-echo SV-wave case was:
0
2
4
6
8
10
0
0.2
0.4
0.6
0.8
1
1.1
Notes: Recall, this again generally agreed with the Kirchhoff approximation but now there were deeper oscillations in the separation of variables solution.

## Slide 68
Flaw Scattering - SDH
Using this separation of variables solutions at many frequencies to synthesize an SV-wave impulse time domain solution (pulse-echo)
The time-domain pulse-echo SV-wave response of a 0.5 mm radius cylindrical void in steel (cp =5900 m/s, cs = 3200 m/sec) obtained by applying a low-pass cosine-squared windowing filter between 10 and 20 MHz to the separation of variables solution and then inverting the result into the time domain with the inverse Fourier transform.
-
1
-
0.5
0
0.5
1
1.5
-
40
-
30
-
20
-
10
0
10
20
30
creeping wave
time,
m
sec
amplitude
-
1
-
0.5
0
0.5
1
1.5
-
40
-
30
-
20
-
10
0
10
20
30
creeping wave
time,
m
sec
amplitude
Notes: Those deeper oscillations are present because the creeping wave response is larger than in the P-wave case.

## Slide 69
Flaw Scattering - SDH
Experimentally determined scattering amplitude by deconvolution (side-drilled hole)
Notes: We mentioned earlier that another way to obtain scattering amplitudes is experimentally. For small flaws we can write the received voltage as a product of the scattering amplitude by a factor G which can be obtained through models and measurements. We will not give the details for obtaining G here but we show some of the general parts of that factor here, including the system function and an integral over the length, L, of the inclusion of the fields incident on the flaw, which we can obtain with beam models. Through deconvolution, then we can obtain the scattering amplitude.

## Slide 70
0
2
4
6
8
10
12
14
16
18
20
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
frequency, MHz
|A/L|
Flaw Scattering -SDH
Notes: Here is the separation of variables pulse-echo P-wave scattering amplitude response for the cylindrical void and the corresponding scattering amplitude determined experimentally over the bandwidth of a 5 MHz transducer. This comparison shows that one of the challenges of NDE testing is that inherently we are always seeing flaw responses over a limited range of frequencies so that limitation often makes it difficult to use features of the response predicted by models.