## Slide 1
Waves Used in NDE
Notes: The waves we have been describing so far are bulk waves. There are a number of other types of waves used in NDE testing which we will also describe here.

## Slide 2
Learning Objectives
Bulk Compressional, Shear Waves
Rayleigh (surface) waves
Lamb (plate) waves
Notes: We will examine some ways that bulk waves are used in NDE and consider briefly some other types of waves such as surface waves and plate waves.

## Slide 3
Compressional and Shear Wave Contact Transducers
fluid couplant
"solid" couplant
P-wave transducer
S-wave transducer
Notes: There are two types of contact transducers. In a P-wave transducer the transducer crystal experiences an expansion and contraction type of motion and transmits a corresponding P-wave with similar motions into the underlying elastic solid. To maintain good coupling to the material a thin fluid couplant layer is normally used. In contrast, an S-wave transducer crystal experiences shearing motions which are transmitted as an S-wave. In this case we must have a semi-permanent type of coupling such as glue between the transducer and the part to transmit this shearing motion. Thus, unlike a P-wave transducer, we cannot move the transducer around on the surface.

## Slide 4
incident
P-wave
reflected
P-wave
transmitted
P-wave (
f)
transmitted
S-wave (
y
)
x
y
r
2
c
p2
c
s2
r
1
c
p1
,
,
,
q
p2
q
s2
q
p1
p1
q
fluid
solid
v
p
inc
v
p
reflt
v
p
trans
v
s
trans
Generalized
Snell's law:
Mode Conversion
Notes: When waves are incident at an oblique angle to an interface one generates both compressional and shear waves whose angles are both controlled by Snell’s law. Here we see an example of such plane waves in an immersion setup

## Slide 5
P
P
S
P
S
P
inhomogeneous
P-wave
inhomogeneous
P, S waves
Critical Angles
qp1
qp1
qp1
(1)
(2)
(3)
first critical angle
second critical angle
Notes: In oblique incidence problems involving elastic solids there are two critical angles present. For a fluid-solid interface case shown we first see the case (1) of the transmitted waves when we are below the first critical angle. In this case both P- and S-waves are transmitted into the solid. However, above the first critical angle the transmitted P-wave becomes an inhomogeneous wave (see (2)) that propagates along the interface and decays exponentially away from that interface, leaving only a transmitted S-wave to propagate in the solid. Above a second critical angle (case (3)) both the P- and S-waves become homogeneous waves traveling along the interface, and no transmitted wave exists in the solid. To have the first critical angle exist we must have cp1 <cp2 and for the second critical angle to exist we must have cp1<cs2

## Slide 6
Angle Beam Shear Wave Transducer
weld inspections
P-wave crystal and backing
plastic wedge
reflected
P- and S-waves
(suppressed)
SV-wave
Notes: We can use critical angle phenomena to generate an angle beam shear wave transducer where we place a P-wave crystal at an angle on a low speed wedge made of a material such as Lucite. This crystal generates primarily a P-wave in wedge which is transmitted as only an SV-wave into the underlying part if the angle is above the first critical angle but below the second critical angle. Again, a thin fluid couplant is used between the transducer and the part. Such angle beam shear wave transducers are commonly used for weld inspections where by moving the transducer back and forth on the surface we can scan different portions of the weld.

## Slide 7
stress-free surface
Rayleigh (Surface)Wave Transducer
Rayleigh wave
angle chosen such that
Notes: If we use an angle beam transducer setup but choose the incident angle so that it is slightly above the second critical angle, then we can generate a combination of inhomogeneous P- and S-waves that produce a Rayleigh wave which can travel for long distances along a stress-free surface. The Rayleigh wave speed (which we discuss shortly) is slightly smaller than the shear wave speed.

## Slide 8
In the late 1800's Lord Rayleigh looked for a wave
confined near the stress-free surface of an elastic solid
of the form:
x
y
Notes: To see how Rayleigh waves arise, consider a combination of inhomogeneous P- and SV-waves traveling along a stress-free surface. Rayleigh took potentials of the form shown above, having a wave speed, c, which at first is unspecified.

## Slide 9
By satisfying the equations of motion
and the stress-free boundary
conditions
on y = 0
Rayleigh found that the wave speed, c, must satisfy
(1)
compressional and shear wave speeds
Notes: By satisfying both the equations of motion and the stress-free boundary conditions, Rayleigh found that wave speed, c, must satisfy the Rayleigh wave speed equation (1).

## Slide 10
Rayleigh's equation
There is always one real root of this equation,
where
Poisson's ratio
The Rayleigh wave travels about 90% of the shear wave speed
A good approximation of this root is:
Notes: Rayleigh’s equation always has a solution c =cR which is slightly smaller than the shear wave speed. The simple approximate expression shown above can often be used to obtain the Rayleigh wave speed.
Rayleigh waves are very useful for applications such as inspecting the surface of parts for surface-breaking cracks since they are very sensitive to such flaws. Rayleigh waves can travel for long distances because, unlike bulk waves, they only spread out on the surface rather than spreading out through the entire volume of the part. They are, however, sensitive to surface conditions such as roughness.

## Slide 11
ux
uy
uy
ux
txx
tyy ,
txy
tyy
txx
txy
displacement
or velocity
stresses
The depth of penetration is a function of the frequency
Notes: Here are some plots of the displacements and stresses in a Rayleigh wave. The exact depth of penertration of the Rayleigh wave is a function of the frequency.

## Slide 12
5 MHz, 6 mm radius transducer on a Lucite wedge radiating into aluminum
0.0
1.0
Vy velocity profile versus distance and depth in the plane z=0
200
20
400
0.5
y (mm)
x (mm)
Notes: This, and the next three slides, will show some simulated wavefields generated by a Rayleigh wave transducer. Here, we see the vertical velocity profile in a vertical plane where red is high amplitude and blue is low amplitude

## Slide 13
1.0
200
20
400
0.5
Vx velocity profile versus distance and depth in the plane z=0
5 MHz, 6 mm radius transducer on a Lucite wedge radiating into aluminum
y (mm)
x (mm)
Notes: Here is the corresponding amplitude in the x-direction

## Slide 14
x, mm
z, mm
Vx/Vo
2-D profile of the Vx velocity component at the surface
5 MHz, 6 mm radius transducer on a Lucite wedge radiating into aluminum
decay of Rayleigh wave ~
Notes: This is a plot of the x-velocity on the stress-free surface. At some distance from the transducer we see that the velocity profile is decreasing in amplitude like one over the square root of the distance, which is smaller than a spherical wave spreading which would be like 1/x.

## Slide 15
20
-20
20
200
400
z, mm
x, mm
Vx velocity component beam profile at the surface
in the plane of the interface
5 MHz, 6 mm radius transducer on a Lucite wedge radiating into aluminum
Notes: Here we are looking directly down on the free surface at the x-velocity wavefield, showing the beam generated from the Rayleigh wave transducer.

## Slide 16
w =2pf … frequency
(rad/sec)
2h
If one looks for solutions of the form
Lamb (Plate) Waves
Notes: If we place an angle beam transducer on a thin plate, we will generate a complex set of multiply reflected P- and SV-waves. These can merge to form a wave, called a Lamb or plate wave, that travels in the thin plate with a frequency dependent wave speed. We can thus try to find solutions for such a wave in the plate which travels with a wave speed, c, and has some variations across the thickness of the plate.

## Slide 17
then solutions of the following two types are found:
extensional waves
flexural waves
10
10
x
y
2h
(b)
(a)
Notes: If we satisfy both the wave equations and the stress-free conditions on the surface of the plate we will find that we can have two types of plate wave disturbances called extensional waves and flexural (bending) wave where the functions f and g have the forms shown.

## Slide 18
+ … extensional waves
- … flexural waves
satisfying the boundary conditions
on
gives the Rayleigh-Lamb equations:
There are multiple solutions of these equations. For each
solution the wave speed, c, is a different function of
frequency. Each of these different solutions is called a "mode"
of the plate.
Notes: The boundary conditions in particular give us the Rayleigh-Lamb equations for the wave speed, c, of the extensional and flexural waves. These equations have multiple solutions where each solution has a different dependency on the frequency. Each of these solutions is called a mode of the plate.

## Slide 19
consider the extensional waves
If we let
(high frequency)
then both tanh functions are
and we find
so we just have Rayleigh waves on both stress-free surfaces:
Notes: If we examine the Rayleigh-Lamb equation for the extensional waves at high frequencies we find the same equation as for Rayleigh waves. In this limit the extensional waves are just Rayleigh waves propagating on both surfaces.

## Slide 20
In contrast for kh <<1 (low frequency)
we find
and the Rayleigh-Lamb equation reduces to
which can be solved for c to give
Notes: At low frequencies, the wave speed of extensional waves become a constant equal to the wave speed for P-waves in a plate.

## Slide 21
frequency-thickness (MHz-mm)
c
c = cR
fundamental
extensional
mode
phase
velocity
(m/s)
c = cplate
Extensional Waves
Notes: Here we show the behavior of the first ten extensional modes in the plate as a function of frequency. Obviously there can be considerable complexity in these results but we will not discuss the details further here as our focus will be primarily on bulk waves.

## Slide 22
frequency-thickness (MHz-mm)
fundamental
flexural
mode
c
phase
velocity
(m/s)
Flexural Waves
c = cR
Notes: Here are the corresponding flexural plate mode curves. At low frequencies we see a much different behavior from that of extensional waves.

## Slide 23
Homework problems
S.3, S.4, S.5
Notes: Special homework problems.