## Slide 1
Ultrasonic System Measurement Model - II
Notes: This will be an overview of the various ultrasonic measurement models that have been developed for NDE tests.

## Slide 2
Learning Objectives
Definition of a Measurement Model
Three Types of Measurement Models
Auld Model
Thompson-Gray
Model for 2D scatterers
Verifying the Modeling Assumptions
and Measurements Needed
Notes: We will define what an ultrasonic measurement model is and give examples of three types of models that have been developed. We will also discuss the steps we can take to verify the various assumptions made and summarize the measurements needed.

## Slide 3
Sf
n
What is an Ultrasonic Measurement Model? A model that expresses the output voltage, vR(t) ,received from a flaw in a ultrasonic testing configuration in a form that explicitly gives the modeling or measurement parameters needed to obtain that voltage (immersion shown only as a specific example)
Pulser
Receiver
surface of the flaw which has an outward normal, n
All the measurement models discussed use VR(w), the frequency components of vR(t)
component being inspected
Ultrasonic Measurement Models
A
B
Notes: An ultrasonic measurement model must predict the measured time domain output voltage in a flaw measurement. Our measurement models will all be constructed in the frequency domain but an inverse FFT will yield the desired output voltage signal.

## Slide 4
Ultrasonic Measurement Models
Electroacoustic Measurement Model - 2002
Dang, C. J., Schmerr, L.W., and A. Sedov," Modeling and measuring all the elements of an ultrasonic nondestructive
evaluation system. I: Modeling Foundations," Research in Nondestructive Evaluation, 14, 141- 176, 2002.
Sf
n
pulser
cabling
sending
transducer
receiving
transducer
cabling
receiver
propagation,
flaw scattering
output voltage
driving voltage
= ?
Notes: We have seen how the pulser/receiver, cabling, and transducer(s) can all be described in terms of components that can either be modeled or measured. Those aspects of the ultrasonic system can all be combined into a single system function, which we have seen can be measured in a calibration experiment. The remaining part of the system, the acoustic/elastic transfer function, tA , involves propagation and scattering of the waves present so it is a key element in the measurement model that must be obtained with models. A model of an ultrasonic system with all the components shown above described completely was first obtained by Dang et. al. in 2002 and called an electroacoustic measurement model

## Slide 5
Auld Electromechanical Reciprocity Relation
Auld (1979) , using reciprocity relations and the solutions to two specific problems, developed an explicit relation that has been widely used
problem (1)
problem (2)
Sf
n
transducer A firing,
flaw present
transducer B firing,
flaw absent
The two problems:
Ultrasonic Measurement Models
B. A. Auld, Wave Motion,, Vol. 1, (1979), pp. 3-10.
A
A
B
B
Notes: In 1979 Bert Auld used reciprocity relations and the solution to two specific problems: problem (1), where the flaw was present in the component being inspected (i.e. the problem we want to solve, and problem (2), the same configuration except where the flaw was absent. With these solutions Auld was able to generate a general model of the ultrasonic measurement process. Auld used a contact testing case, rather than the immersion case shown here, in his relations but that difference is not significant.

## Slide 6
Sf
n
Auld Electromechanical Reciprocity Relation
dG… change in cable transmission coefficient due to the presence of the flaw
P… power delivered by the transducer
stress vector and velocity for problem (1) : A firing and flaw present
stress vector and velocity for problem (2): B firing and flaw absent
Ultrasonic Measurement Models
A
B
Notes: Auld showed that a change in the signal carried by the cable at the receiver could be expressed in terms of an integral over the flaw surface of the fields in problems (1) and (2).

## Slide 7
Sf
n
Auld Electromechanical Reciprocity Relation
Auld's assumptions:
1) linear, reciprocal electromechanical system (harmonic disturbances)
2) fundamental TEM mode propagating in the cable
Since we expect
Auld's relation "essentially" is
an ultrasonic measurement model
Ultrasonic Measurement Models
A
B
Notes: Since we expect the change in signal in Auld’s model to be directly related to the received voltage signal, Auld’s relation is “essentially” a measurement model. It is a very general model since it only assumes that the measurement system is linear and reciprocal and that the electrical disturbances in the cable are propagating TEM mode waves, which are typically the fundamental waves present in coaxial cables.

## Slide 8
An Alternative Reciprocity Relation
In 1998, Dang, Schmerr, and Sedov obtained a completely explicit model relationship using a purely mechanical reciprocity relationship plus several other relatively weak assumptions
problem (1)
problem (2)
vA
(1)
Sf
vB
(2)
n
Ultrasonic Measurement Models
A
A
B
B
Notes: In 1998 Dang et. al. used purely mechanical reciprocity relations to characterize the acoustic/elastic transfer function and arrive at a form that is similar to the ones we have been discussing where the system function appears directly. This is now indeed an ultrasonic measurement model of the Auld form which explicitly expresses the output voltage in terms of the system parameters. Henceforth, we will call this model Auld’s measurement model in recognition of his foundational contributions.

## Slide 9
… system function (pulser, cabling, receiver)
… average velocity over the face of transducer A in problem (1)
… average velocity over the face of transducer B in problem (2)
… radiation impedance of transducer A in problem (1)
Ultrasonic Measurement Models
Notes: Here are the basic elements appearing in this form of Auld’s measurement model

## Slide 10
assumptions used to obtain this explicit model
1) linear, reciprocal acoustic and elastic media (harmonic disturbances)
Ultrasonic Measurement Models
Auld’s Measurement Model
Notes: Like Auld’s original model, this form relies on very few assumptions. First, there is the assumption that the waves in the system satisfy acoustic/elastic reciprocity.

## Slide 11
average velocity
2) we also assumed the output velocity for the transducers can be written in a separable form. For transducer A, for example
Here, the "forces" are defined in terms of weighted pressure integrals over the transducer face, using the same functions used to describe the velocity. For example, for transducer A
density, wave speed of the fluid
For a piston transducer
Ultrasonic Measurement Models
A
Notes: Second, the velocity on the face of the transducers was assumed to be in a separable form where there is a spatial variation terms and a frequency dependent term . This form is satisfied, for example, by a piston transducer, which is a commonly used transducer model.

## Slide 12
flaw
Ft
FB
Transmitted
force
Blocked
force
A
B
These two assumptions lead to an explicit expression for the acoustic/elastic transfer function:
Notes: With these two assumptions we can obtain an explicit expression for the acoustic/elastic transfer function in terms of an integral over the flaw surface of the fields appearing in problems (1) and (2).

## Slide 13
3) we also assume that the pulser, receiver, transducers and cabling can be replaced by equivalent linear, time-shift invariant (LTI) systems, i.e.
Then, we can write the reciprocity relationship in the form
or, finally
Ultrasonic Measurement Models
Notes: We also assume that all the other parts of the system can be represented as LTI systems and that we can lump all those parts into a system function.

## Slide 14
assumptions
1) linear, reciprocal acoustic and elastic media (harmonic disturbances)
2) the output velocity for the transducers can be written in a separable form
3) the pulser, receiver, transducers and cabling can be replaced by equivalent linear, time-shift invariant (LTI) systems.
A General Ultrasonic Measurement Model
Ultrasonic Measurement Models
Notes: This, then is a general ultrasonic measurement model based on very few assumptions.

## Slide 15
4) if we also assume that the transducers behave as piston radiators at high frequency then
and our explicit model becomes, finally
Ultrasonic Measurement Models
Notes: The radiation impedance can normally be taken as its high frequency value, yielding the model shown. This model can be used in essentially the same form for contact testing as well as immersion testing and can include other setups such as angle beam transducers.

## Slide 16
5) now, assume the incident waves are quasi-plane waves in the vicinity of the flaw, e.g.
and also define normalized amplitudes of these quasi-plane waves as
Ultrasonic Measurement Models
Notes: Now, let’s assume that the waves incident on the flaw can be describes as quasi-plane waves and normalize the velocity wavefields of these waves by the velocities on the faces of the transducers. Note that we can model these normalized fields with ultrasonic beam models without having to know the amplitudes of the actual velocities present on the transducer faces.

## Slide 17
Then the form of the measurement model becomes
Ultrasonic Measurement Models
velocity fields
in problems (1),(2)
due to unit average velocities on the transducer faces
scattered wave fields
from the flaw
Notes: Then the form of the measurement model becomes as shown here, where the velocity fields and scattered wave terms all can be described directly with models.

## Slide 18
the normalized fields are defined as velocity and stress in
problem (1) due to an incident wave of unit displacement amplitude
The flaw scattering term is rather complex:
stresses and velocity components in problem (1)
components of the incident wave direction and polarization
in problem (2)
components of the unit outward normal to the flaw surface
elastic constants tensor
Notes: The scattering terms are rather complex functions of the fields on the surface of the flaw. They are computed here as the scattered waves due to an incident wave of unit displacement amplitude so they can be calculated independent of the actual amplitudes of the incident waves, which are contained in the normalized velocity terms. The incident wave is taken to be of unit displacement amplitude since most plane wave scattering amplitudes in elastic solids are defined for such an incident wave.

## Slide 19
rs
n
flaw
U0
U0 … displacement
amplitude for wave
of type b (b = P,S) in
problem (1)
Scattered wave of
type a (a = P,S)
3-D scattering amplitude
incident wave with polarization
da in problem (2)
scattered displacement
from a flaw
P-wave
S-wave
Ultrasonic Measurement Models
Notes: Recall the scattered displacements in the far field of the flaw can be described in terms of scattering amplitudes. Also note that if the receiving transducer acts a sending transducer it will generate waves with a polarization vector dP or dS at the flaw. This polarization vector is important, as we will see.

## Slide 20
However, it can be shown that
3-D scattering amplitude
vector scattering amplitude of waves in problem (1)
polarization vector of incident
waves in problem (2)
Ultrasonic Measurement Models
Notes: The component of the scattering amplitude in the negative dP or dS direction can be shown to be an integral over the surface of the flaw of a scalar function that appears in the measurement model.

## Slide 21
Measurement Model - Quasi-Plane Waves
Ultrasonic Measurement Models
The beam velocity terms and flaw scattering terms appear separately in this model but they still must be combined before the voltage can be obtained
Notes: Thus, the measurement model can be written in terms of the normalized velocity fields and this scalar flaw scattering term.

## Slide 22
6) Now, assume a small 3-D flaw, i.e. where the incident waves do not vary significantly in amplitude over the surface of the flaw
O
Then
and, recall
Notes: If we now assume that the flaw is small enough so that the velocity fields do not vary significantly over the flaw surface, then these velocities can be taken out of the integral and the remaining integral is a scalar scattering amplitude term that is the specific component of the vector scattering amplitude defined previously.

## Slide 23
Measurement Model (Thompson-Gray form)
beam models
plane wave far field
scattering amplitude
component
Ultrasonic Measurement Models
R. B. Thompson and T. A. Gray, J. Acoust. Soc. Am., Vol. 74, (1983), pp. 140-146.
acoustic/elastic
transfer function
Notes: This final form is then in a form due to Thompson and Gray called the Thompson-Gray measurement model. A very important feature of this model is that the flaw scattering response is separate from the other terms so that in principle it gives us a way to extract flaw information from the measured ultrasonic signals through deconvolution. In contrast, in the Auld model the scattered waves due to the flaw and transducer(s) wave fields are intermixed. Note that the original derivation of the Thompson-Gray model did not identify the scalar scattering amplitude as an explicit component of the vector far field scattering amplitude, as we have done here.

## Slide 24
Measurement Model (Thompson-Gray form)
1) linear, reciprocal acoustic and elastic media (harmonic disturbances)
2) the output velocity for the transducer(s) can be written in a separable form
3) the pulser, receiver, transducers and cabling can be replaced by equivalent linear, time-shift invariant (LTI) systems.
4) the transducers are assumed to behave as piston radiators operating at high frequency
5) the incident waves are quasi-plane waves in the vicinity of the flaw
6) the scatterer is a small 3-D flaw where the incident waves do not vary significantly in amplitude over the surface of the flaw
Ultrasonic Measurement Models
Notes: Here is the Thompson-Gray model and the assumptions that it is based on.

## Slide 25
6a) If instead, the scatterer is a small cylindrical flaw (e.g. side-drilled hole), with incident and scattered wave directions in the plane of the cross-section then we can assume
only
In this case
O
Ultrasonic Measurement Models
Notes: For small two-dimensional flaws such as side drilled holes we can again make the assumption that the incident and scattered fields lie basically in a plane perpendicular to the axis of the “flaw” but the incident wave fields will vary along that axis so that we must integrate the incident velocity fields along that axis and the scattering term reduces to a line integral around the cylinder in a plane perpendicular to that axis.

## Slide 26
3-D scattering amplitude component of a 2-D, cylindrical geometry (end effects neglected) is just
so that the measurement model can be expressed, finally, as
Ultrasonic Measurement Models
Schmerr, L.W., and A. Sedov, "Modeling ultrasonic problems for the 2002 benchmark session,"
Review of Progress in Quantitative Nondestructive Evaluation, D.O. Thompson and D.E. Chimenti, Eds.,
American Institute of Physics, Melville, N.Y. , 22B,1776-1783, 2003.
Notes: The 3-D scattering amplitude component of a 2-D scatterer of length L with the end effects neglected can be written as shown and the measurement model is in the form given.

## Slide 27
Relationship between 2-D and 3-D scattering amplitudes
which gives the alternate form
Ultrasonic Measurement Models
Notes: Many model studies of cylindrical scatterers treat the scattering problem as a purely 2-D problem described by a 2-D scattering amplitude in the far field. We can relate such 2-D model results to our scattering problem, which is inherently 3-D in nature and write the measurement model in terms of a scalar 2-D scattering amplitude instead if we so desire.

## Slide 28
1) linear, reciprocal acoustic and elastic media (harmonic disturbances)
2) the output velocity for the transducer(s) can be written in a separable form
3) the pulser, receiver, transducers and cabling can be replaced by equivalent linear, time-shift invariant (LTI) systems.
4) the transducers are assumed to behave as piston radiators operating at high frequency
5) the incident waves are quasi-plane waves in the vicinity of the flaw
6) the scatterer is cylindrical flaw with incident and scattered wave directions in the plane of the cross-section, where the incident waves do not vary significantly in amplitude over the small cross-section of the flaw
Measurement Model for 2-D scatterers
Notes: Here is the Thompson-Gray type of measurement model for 2-D scatterers and the assumptions on which it is based.

## Slide 29
2-D small flaw (Schmerr-Sedov form)
3-D small flaw (Thompson-Gray form)
General Measurement Model (Auld form)
Ultrasonic Measurement Models
Notes: In summary, we have three types of measurement models: (1) the Auld type of model that is applicable to a very wide range of problems and flaws, (2) a Thompson-Gray type of model suitable for the inspection of 3-D small flaws, and (3) A Thompson-Gray type of model developed by L. Schmerr and A. Sedov that is suitable for 2-D scatterers such as side-drilled holes.

## Slide 30
Is the system linear and reciprocal?
Electrical linearity checks of pulser/receiver
A
A
A
Using Measurement Models
Ultrasonic Measurement Models
Cabling reciprocity checks
For a transducer, reciprocity implies the voltage and current measurements
when it is being used as a sender and receiver must be related:
Notes: Linearity and reciprocity are two key assumptions in all the ultrasonic measurement models. We can, of course, do linearity checks on the pulser/receiver (and such checks are sometimes specified in inspection protocols). We have seen how to check reciprocity for our cable measurements. We can examine a transducer acting as a sender and receiver, as shown, and check its reciprocity with the relationship given above for the measured electrical signals. This relationship comes from writing the ratios V/I and Is/Vinf in terms of the 2x2 transfer function components for the transducer on transmission and reception and assuming those components satisfy reciprocity. In that case these ratios are equal, leading to the above expression ).

## Slide 31
Is the transducer acting as a piston?
Compare responses with theoretical predictions in a reference experiment, e.g.
Is a quasi-plane wave assumption valid?
Compare
with
as computed with a non-paraxial beam model
Ultrasonic Measurement Models
Notes: We can also check to see if a piston transducer model is appropriate by, for example, moving a small reflector along the axis of the transducer and comparing the on-axis fields with those predicted by a piston transducer model. For a Thompson-Gray type of model, which relies on the quasi-plane assumption, we could check the validity of that assumption by comparing the fields found in a general Auld type of model with the reduced forms appropriate for a quasi-plane wave (paraxial) model.

## Slide 32
Is a small flaw assumption valid?
Compare
with
(3-D case)
or
(cylindrical case)
Ultrasonic Measurement Models
Notes: The Thompson-Gray model also assumes the fields do not vary significantly over the flaw surface so that assumption can also be checked by a comparison with the more general underlying model terms.

## Slide 33
What supporting measurements are needed?
System factor
Obtain in separate experiment
Velocity, Attenuation
Obtain in separate experiments
Transducer effective radius, focal length
Ultrasonic Measurement Models
Obtain in separate experiments
Notes: An ultrasonic measurement model also relies on a number of supporting measurements. These include measurements of velocity and attenuation in the materials being inspected and the measurement of the system function (or its underlying components if we want to do a more in-depth characterization of the system as we have discussed). The transducer effective radius and focal length are also parameters that can be measured.

## Slide 34
Summary
A measurement model form is available suitable for simulating most NDE inspections
To make these models useful one needs to have
ultrasonic beam models
flaw scattering models
experimental determination of essential parameters
Once all these elements are available one has a very powerful tool for designing tests, optimizing components, and replacing expensive experimental procedures.
Ultrasonic Measurement Models
Notes: The measurement models we have discussed give us the capability to model many NDE experimental setups. These models can both be used as design tools and for understanding the signals seen in ultrasonic tests.